## Slide 1: BASIC GEOTECHNICAL ENGINEERING

## Slide 2: MODULE 2: Syllabus
Soil Structure and Clay Mineralogy Single grained, honey combed, flocculent and dispersed structures, Valence bonds.
Soil-Water system, Electrical diffuse double layer, adsorbed water, base-exchange capacity, Isomorphous substitution.
Common clay minerals in soil and their structures- Kaolinite, Illite and Montmorillonite and their application in Engineering

## Slide 3: INTRODUCTION
The arrangement of soil particles with respect to one another is known as soil structure.
The soils in nature have different structures depending upon the particle size and mode of formation.
Soil structure is an important factor which influences many soil properties such as permeability, compressibility and shear strength.

## Slide 4
Soil structures are generally recognized as:-
Single grained structures
Honey combed structures
Flocculent structures
Dispersed structure
Coarse Grained Skeleton structure
Cohesive matrix structure

## Slide 5: SINGLE GRAINED STRUCTURES
Coarse grained soils (diameter > 0.02mm) settle out of suspension in water as individual grains independently of other grains.
The major force causing their deposition is gravitational and surface forces which are too small to be of practical importance.
The weight of the grains causes them to settle, and get particle to particle contact on deposition.
They may be deposited in a loose state having a void ratio or in a dense state having a low voids ratio.

## Slide 6: HONEY COMBED STRUCTURE

## Slide 7
Honey combed structures exists in grains of silts or rock flour smaller than 0.02 mm diameter larger than 0.02 mm.
When such grains settle under gravity the surface forces also play an equally important role.
The surface forces at the contact areas as the grains comes in contact at the bottom of suspension, are large enough compared to the submerged weight to prevent the grains from rolling down immediately into positions of equilibrium among the grains already deposited.
The grains coming in contact are held until miniature arches are formed, bridging over relatively large void spacing and forming a honeycomb structure.
Each cell in structure made up of numerous single mineral grains. The structure so formed has high voids and is capable of carrying relatively heavy loads without excessive volume change.

## Slide 8: FLOCCULENT STRUCTURE
Clay consisting of very fine particles or colloids may have two types of structures i.e. flocculated or dispersed.
Lambe explained a structure of clay from colloidal chemical viewpoint. According to him a flocculated structure of clay platelets is formed when there are edge to edge contacts between the platelets as shown in fig below.
A structure is formed if the net electrical forces between adjacent soil particles at the time of deposition are attraction forces.
If there is a connection of dissolved minerals in the water (Eg:- Marine water) the tendency of flocculation is increased.
Clay having a flocculent structure has a high voids ratio.

## Slide 9: DISPERSED STRUCTURE
A dispersed or oriented structure is formed when the platelets having face to face contact which is more or less parallel.
Such as structure is formed if the net electrical forces between adjacent soil particles at the time of deposition are repulsion.
In dispersed structure the volume of voids are relatively less, have a high shear strength, high compressibility and low permeability.

## Slide 10: COARSE GRAINED SKELETON STRUCTURE
It can be found in the case of composite soils in which the coarse grained fraction is greater in proportion compared to fine grained fraction.
The coarse grained particles forms the skeleton with particle to particle contact and the voids between the particles will be occupied by fine grained particles.

## Slide 11: COHESIVE MATRIX STRUCTURE
These structures can be found in composite soils in which the fine grained fraction is more in proportion compared to coarse grained fraction.
In this case the coarse grained particles will be embedded in fine grained fraction and will prevent from having particle to particle contact.

## Slide 12: BONDING FORCES
In order to understand the structure of the soil particles and soil masses, the basic knowledge about the inter-atomic and intermolecular bonding forces is very essential. The atomic bonds can be broadly grouped into two types namely:
Primary valence bonds
Secondary valence bonds

## Slide 13: PRIMARY VALENCE BONDS
These are the strong bonds that hold the atoms together.
Only the outer shell electrons participate in the formation of these bonds.
Primary valence bonds are off three types:
Covalent bonds
Ionic bonds
Metallic bonds

## Slide 14: COVALENT BONDS
If one or more bonding electrons are shared by two atomic nuclei, so that they are served to complete the outer shell of both the atoms, such bonds are termed as covalent bond.
Example: - In a water molecule, each hydrogen atom (H) shares an electron (yellow) with the oxygen atom (O).

## Slide 16: IONIC BONDS
These are results from the electrostatic attraction between ‘+ve ion’ (Cations) and ‘–ve’ (Anions) formed from the free atoms through loss or gain of electrons respectively.
Cations: - Metals, alkalis (Sodium & Potassium), alkaline (Calcium & Magnesium)
Anions: - Chlorine, Iodine & Oxygen

## Slide 17: IMPORTANT POINTS
Primary valence bonds are very strong.
If the centre’s of positive and negative charges coincides then that system is called non polar system.
If the centers of positive and negative charges don’t coincides then that system us called polar system & a molecule exhibiting such characteristics are called a dipole. If ‘e’ is the charge & the ‘L’ is the distance between the center of ‘+ve’ and ‘-ve’ charges, then the moment ‘e ×L’ is known as dipole moment.
Dipole tends to orient in a electric field & they behave like permanent magnets.

## Slide 18: METALLIC BOND
It is a type of chemical bonding that arises from the electrostatic attractive force between conduction electrons & positively charged metal ions.
It has 1 to 3 electrons in outer shell and bond between these electrons and nucleons is very weak.

## Slide 19: SECONDARY VALENCE BONDS
These are weak bonds that link the molecules together.
They are off two types namely:
Hydrogen Bond
Vander Waals Bond

## Slide 20: HYDROGEN BOND
Attraction exists between oppositely charged ends of two permanent dipole and if the hydrogen is the ‘+ve’ end of the dipole, then the resulting bond is known as Hydrogen bond.
Permanent bonds like hydrogen bonds are directional bonds.
Hydrogen bond is stronger than other types of secondary valence bonds & plays an important role in interaction between soil particles & water.
Ex: - Water

## Slide 22: VANDER WAALS BOND
The fluctuating dipole bonds are known as Vander Waals bonds.
At any time there may be electrons at one side of the atomic nucleus than the other.
In such cases weak instantaneous dipole whose oppositely charge ends attract each other are formed.
The vander waals bonds are non directional.

## Slide 23: SOIL WATER SYSTEM
Water present in pore spaces of soil is termed as soil water or pore water. The quantity of water present in the pores will significantly influence its physical, chemical and engineering properties.
It can be classified as: -
Free water or Gravitational Water
Held water or Environmental water

## Slide 24
Free water or Gravitational water: It flows freely under gravity, under some hydraulic gradient and are free from surface forces exerted by the soil particles. This water can be removed by oven drying method.
Held Water or Environmental Water: It is held under the influence of surface forces such as electrochemical forces or other physical forces.
Both type of water are important in geo-environmental engineering. The mechanism of soil held water interaction is complex and influenced by soil type, mineralogy, current and past environmental condition and stress history.

## Slide 25: TYPES OF HELD WATER
Structural water: It is present within the crystal structure of mineral.
Capillary water: Water that remains in the soil after gravitational water is drained out that is subjected to capillary movement and that is in the form of film around the soil grains.
Adsorbed water:
It is strongly attracted to soil mineral surfaces especially clays. The clay particles are negatively charged; when dry particles are exposed to humid atmosphere they attract water molecules which are dipole in nature to stick to them.
This water which is adsorbed by the clay particles from the surrounding atmosphere is known as hydroscopic moisture content of the soil.
This can be removed by heating the soil mass to 1050C – 1100C in an oven for 24 hrs.

## Slide 26
When dry charged clay platelets are put in water, water molecules adhere to the clay surface due to many mechanisms.
1. Hydrogen Bond: Hydrogen atoms of water molecules are attracted to the oxygen or hydroxyl atom on the surface of the clay particles.

## Slide 27
2. Clay Dipole Attraction: Water molecules being dipole orient with their positive ends towards the negative charge of clay surfaces.

## Slide 28
3. Attraction by Osmosis
Water being an electrolyte contains many cations. These cations are strongly attracted to the negatively charged clay surfaces. Due to their specific sizes the cations are arranged near the clay surface in such a way that their concentration defuse away from the surface till the cation concentration become equal to that in free water medium. The negatively charged clay surface and the defused water layer with cations together constitute “diffused double layer”.

## Slide 29: DIFFUSE DOUBLE LAYER (DDL)

## Slide 30
It is an ionic structure that describes the variation of electric potential near a charged surface, such as clay, and behaves as a capacitor.
Formation: Clays are aluminosilicates in which some of the aluminum and silicon ions are replaced by elements with different charge.
The diffused double layer water has more density & more viscosity than free water.
The thickness of the diffused double layer is:
More with cations of lower valency
More with less cation concentration in aqueous medium
More with a medium of higher dielectric constant.
When two clay particles tend to approach each other their diffused double layers interact with each other & a strong repulsion develops between them. Hence the particles tend to separate from one another. This is called as double layer swelling of clays. This is more dominant in soils containing montmorillonite clay minerals.

## Slide 31: ISOMORPHOUS SUBSTITUTION
The process of replacing one structural cation for another of similar size is referred to as isomorphous substitution. This replacement represents the primary source of both negative and positive charges in clay minerals.
(OR)
Isomorphic substitution is the replacement of one atom by another of similar size in a crystal lattice without disrupting or changing the crystal structure of the mineral.

## Slide 33: CATION EXCHANGE CAPACITY
It is also known as “Base Exchange Capacity”. Isomorphous substitution gives the clay particle a net negative charge.
To preserve the electrical neutrality cations are attracted towards the clay surface and adhere to the clay surface.
These cations are called exchangeable cations and cations of one type may be replaced by cations of another type.
The quantity of exchangeable cations required to balance the charge deficiency of clay particle is termed as ‘Cation Exchange capacity’ or ‘Base Exchange Capacity’ and it is usually expressed as m eq/100g (milli equivalent/ 100 gms).

## Slide 34
The below table gives the ‘Cation Exchange Capacity’ of typical clay minerals:
Clay Mineral | CEC (m eq/100g)
Kaolinite | 3 – 15
Illite | 10 – 40
Montmorillonite | 80 - 150

## Slide 35: SPECIFIC SURFACE
Specific surface of soil particles is the ratio of surface area of the material to its mass.
It is inversely proportional to the particle size smaller the particle size.
Smaller the particle size more will be the specific surface.
It is proved in the above discussion that clay platelets have negative surface charges to, these negative charges on the clay surface control the behaviour of clays and in turn of the soil.
Clays having more specific surface have more surface charges and hence are more active.

## Slide 36
Clay Minerals | Specific Surface (m2/g)
Kaolinite | 10 - 20
Illite | 80 – 100
Montmorillonite | 800
Following table gives the specific surface of different clay minerals:

## Slide 37: COMPOSITION OF SOILS
The solid portion of soil containing varying amount of crystalline clay and non clay minerals, non crystalline clay minerals, organic matter and precipitated salts.
The term clay means small crystalline particles of one or more number of small groups of minerals; they are basically hydrous alluminus silicate.
As the soils are the products of weathering of rocks, the soil forming minerals are those which are more resistant to physical and chemical weathering.
Rocks + water → Clay, which is formed at or near the surface of the water.

## Slide 38
Clay Minerals: -
The clay minerals that are commonly found in soils belong to a mineral family known as “Phyllosilicates”.
They are sheet or layered structure having a characteristic of stacking arrangements.
The two building blocks/ basic units of all clay minerals are ‘silicon tetrahedron’ and ‘aluminium or magnesium octahedron’.
Clay mineralogy is the science dealing with the structure of clay minerals in microscopic molecular and atomic scale. It also includes the study of mineralogical composition of electrical properties of the clay particles.

## Slide 39: BUILDING BLOCKS
Silicon Tetrahedron: - This unit has a silicon ion tetrahedrally coordinated with ‘4’ oxygen ions & it is symbolically represented as

## Slide 40
Aluminium/ Magnesium Octahedron: - This unit has ‘1’ aluminium or magnesium ion octahedrally coordinated with ‘6’ oxygen or ‘6’ hydroxyls ions and it is symbolically represented as,

## Slide 41
SILICA SHEET
In most of clay mineral structures, silica tetrahedral units occur in a sheet form where 3 of the 4 oxygen’s of each tetrahedron are shared to form a hexagonal net.
The bases of the tetrahedral are all in the same plane & the tips point in the same direction.

## Slide 42
The silica sheets are schematically represented as,

## Slide 43
OCTAHEDRAL SHEET
Like silica sheet, octahedral units can also exist in the sheet form.
Here each hydroxyl ion is common to 2 or 3 octahedral units.
If the aluminium ion is the cation present in the octahedral sheet then the sheet is called ‘Gibbsite sheet’ or ‘aluminium octahedral sheet’.
As the cation is trivalent (Al3+) in the gibbsite sheet only 2/3rd of the possible cation spaces are normally filled and the structure is known as “dioctahedral sheet”.

## Slide 44
Schematically Gibbsite sheet is represented as,

## Slide 45
If the cation present in the octahedral sheet is magnesium then the sheet is called ‘Brucite’ or’ ‘Magnesium Octahedral sheet’.
In this case as the cation is divalent ‘Mg2+’ all possible cation positions are normally filled and the structure is called ‘trioctahedral sheet’.
Schematically Brucite sheet is represented as,

## Slide 46: CLAY MINERALS
The clay minerals have silica sheets & octahedral sheets (Gibbsite or Brucite or both) arranged in some specific combination.
They can be classified according to their crystal structure and stacking arrangements of layers. The members of the same group have somewhat similar engineering properties.
There are 3 types of clay Minerals:-
Kaolinite Clay
Montmorillonite Clay
Illite Clay.
All the clay minerals have 2 basic atomic sheets i.e, Silica tetrahedron sheet and Aluminium Octahedron sheet.

## Slide 47: KAOLINITE (1:1 & TWO LAYER MINERALS)
It is a two layer clay mineral whose unit cell made up of a ‘Silica sheet’ & a ‘Gibbsite sheet’.
Here all the tips of the tetrahedron point in the same direction towards the centre of the unit cell.
These tips of the silica tetrahedron & one of the planes of atoms of gibbsite together forms common plane.
In the common plane 2/3rd of the atoms of oxygen are shared by both silica & octahedral cations.
The remaining atoms in the common plane are hydroxyls and they are located in such a way that each hydroxyl is directly below the hole in the hexagonal head/unit formed by the basis of the silica sheet.

## Slide 48
The theoretical structural formula of Kaolinite is :
The schematic representation of Kaolinite clay mineral units is shown below

## Slide 49
The linkage between 2 basic units of Kaolinite clay mineral is through hydrogen bond and the vander waals forces.
Since the hydrogen bond is relatively strong, it is difficult to separate one basic unit from the other. Therefore Kaolinite clay mineral is quiet stable.
Water cannot enter between the unit cells to cause swelling. Hence Kaolinite is also known as “Non expanding Lattice” type of clay mineral.
The thickness of the Kaolinite particles varies in the range 100 A0 – 1000A0 and the lateral dimension vary in the range 1000A0 to 10000A0.

## Slide 50
Isomorphous Substitution in Kaolinite: -
The Isomorphous substitution in Kaolinite clay mineral is very small.
In Kaolinite it takes place in silica sheets. One Silica ion in every 400 is replaced by one Aluminium ion. This results less surface charge deficiency.

## Slide 51
Origin of Kaolinite Clay Mineral: -
Most Kaolinite is formed primarily from feldspars & mica by acid rocks (Granitic rocks).
Their formation is favoured when alumina is abundant and silica is scarce. This in the case when the electrolite content is less, pH is low & ions tending to flocculate silica are removed by leaching.
The climatic conditions favouring the formation of Kaolinite clay mineral are:
Relatively high precipitation to ensure leaching of cations and oxidation of ions.
Good drainage of the area for the removal of the leached out cations.

## Slide 52
2:1 Clay minerals (Three layered minerals)
These minerals are also known as “Smectite” minerals.
These minerals have their basic units consisting of an “Octahedral sheet” sandwitched between two silica sheets as shown in fig.

## Slide 53: MONTMORILLONITE
This is an important member of Smectite group of clay minerals.
The basic units of this clay mineral consist of 2 silica sheet with a central gibbsite sheet.
The tips of all the silica tetrahedron point towards the centre of the basic units.
The oxygen forming the tips of the tetrahedron are common to all the octahedral sheet & also the remaining anions in the octahedral sheet that fall directly above or below hexagonal holes formed by the bases of silica tetrahedra or hydroxides.

## Slide 54
The theoretical structural formula of Montmorillonite is
The schematic representation of Montmorillonite clay mineral units is shown below.

## Slide 55
The bonding between successive units of Montmorillonite mineral is by Vander Waals force & exchangeable Cations.
This bond is very weak; water can easily enter between the adjacent unit cells causing them to separate.
This results in significant swelling of the clay mineral. Hence Montmorillonite clay mineral is known as expanding lattice type of clay mineral.
The thickness of the clay mineral is about 9.6 A0 & the lateral dimensions vary in the range of 1000 A0 – 5000A0.

## Slide 56
Isomorphous Substitution: -
There is extensive Isomorphous Substitution in Montmorillonite clay mineral and it takes place in octahedral sheet.
Every 6th aluminium ion is replaced by magnesium ion. This results in many large surface charge deficiencies.
Expansive clays such as Bentonite & Black cotton soil have Montmorillonite clay mineral in that.

## Slide 57
Formation of Montmorillonite Clay mineral: -
The parent material for the formation of Montmorillonite clay mineral are those rocks which are rich in alkaline earth’s such as basic & intermediate igneous rocks, volcanic ash & derivatives containing ferromagnesium minerals.
The climatic condition which favors the formation of Montmorillonite clay is:-
Extensive disintegration.
Evaporation exceeding the precipitation.
Poor leeching.
High pH & electrolite content.
Presence of Magnesium & Calcium ions more than Sodium & Potassium ions.

## Slide 58: ILLITE
This is also a 3 layer clay mineral which has two silica sheets with a Gibbsite sheet in between.
However in Illite every 7th silicon ion is replaced by aluminium as a consequence of Isomorphous Substitution.
The resulting charge deficiency is balanced by non-exchangeable potassium ions in between the unit layers.

## Slide 59
The bonding between two unit layers is off Vander Waals force & non exchangeable potassium linkage.
The bonding even though weaker than hydrogen bonding, stronger than Vander Waals forces that exists in Montmorillonite.

## Slide 60
The thickness of Illite particle is in the range of 50A0 to 500 A0 & the lateral dimensions vary in the range of 1000A0 – 5000A0.
The theoretical structural formula of Illite in the absence of Isomorphous Substitution is:

## Slide 61
Formation of Illite Clay mineral: -
Acid Igneous & Metamorphic rock & their derivatives are the usual parent rocks.
For the formation of Illite, presence of potassium is very essential other conditions favorable for the formation of Montmorillonite clay minerals are required for the formation of Illite also.
In addition to crystalline clay minerals soils are composed of non – crystalline silicate clay minerals known as allophones.
These are amorphous in nature, do not have definite composition or shape and they exhibit wide range of physical properties.

## Slide 62: COMPACTION

## Slide 63
Compaction is the process of increasing the bulk density of a soil or aggregate by driving out air.
For any soil, at a given compactive effort, the density obtained depends on the moisture content.
An “Optimum Moisture Content” exists at which it will achieve a maximum density.
Compaction is the method of mechanically increasing the density of soil.

## Slide 64
The densification of soil is achieved by reducing air void space.
During compaction, air content reduces, but not water content It is not possible to compact saturated soil.
It should be noted that higher the density of soil mass, stronger, stiffer, more durable will be the soil mass.

## Slide 65
Increases density
Increases strength characteristics
Increases load-bearing capacity
Decreases undesirable settlement
Increases stability of slopes and embankments
Decreases permeability
Reduces water seepage
Reduces Swelling & Shrinkage
Reduces frost damage
Reduces erosion damage
Develops high negative pore pressures (suctions) increasing effective stress

## Slide 67
Optimum Moisture Content (OMC) is the moisture content at which the maximum possible dry density is achieved for a particular compaction energy or compaction method.
The corresponding dry density is called Maximum Dry Density (MDD). Water is added to lubricate the contact surfaces of soil particles and improve the compressibility of the soil matrix.
It should be noted that increase in water content increases the dry density inmost soils up to one stage (Dry side). Water acts as lubrication.
Beyond this level, any further increase in water (Wet side)will only add more void space, thereby reducing the dry density.
Hence OMC indicates the boundary between the dry side and wet side. Hence the compaction curve as shown in figure indicates the initial upward trend up to OMC and the down ward trend.

## Slide 68: REASONS FOR THE SHAPE OF CURVE
On dry side of OMC, clayey soil shows high suction, lumps are difficult to break or compact.
Increasing the water content reduces suction, softens lumps, lubricates the grains for easy compaction.
As water content increases, lubrication improves compaction resulting in higher dry density.
Now nearly impossible to drive out the last of the air – further increase in water content results in reduced dry density (curve follows down parallel to the maximum possible density curve – the Zero Air Voids curve)

## Slide 69
MDD and OMC depend on the compaction energy and are not unique soil properties.
For sand, suction at low water contents also prevents compaction (but not if completely dry)
In cohesion less soils, MDD is achieved either when completely dry, or when completely saturated.
At low water content, grains are held together by suction (water at grain contacts only)
This prevents compaction.
Laboratory test for MDD on sand requires fully saturated sample, and involves vibration

## Slide 70: COMPACTION TYPES

## Slide 71: STANDARD PROCTOR’S COMPACTION TEST
Refer IS 2720 – Part VII – 1987
Apparatus
Cylindrical metal mould with detachable base plate (having internal diameter 101.6 mm, internal height 116.8 mm and internal volume 945000 mm3)
Collar of 50 mm effective height
Rammer of weight 2.5 kgf (25 N) with a height of fall of 304.8 mm

## Slide 72: PROCEDURE
About 3 kg of dry soil, with all lumps pulverized and passing through 4.75 mm sieve is taken.
The quantity of water to be added in the first trial is decided. (Less for Corse grained soil and more for Fine grained soil).
Mould without base plate & collar is weighed
The inner surfaces of mould, base plate and collar are greased.
Water and soil are thoroughly mixed.
Soil is placed in mould and compacted in three uniform layers, with 25 blows in each layer. Blows are maintained uniform and vertical and height of drop is controlled.

## Slide 73
After each layer, top surface is scratched to maintain integrity between layers.
The height of top layer is so controlled that after compaction, soil slightly protrudes in to collar.
Excess soil is scrapped.
Mould and soil are weighed (W)
A representative sample from the middle is kept for the determination of water content.
The procedure is repeated with increasing water content.
The number of trials shall be at least 6 with a few after the decreasing trend of bulk density.

## Slide 74
DIFFERENCE B/W COMPACTION TYPES

## Slide 75: COMPACTIVE ENERGY

## Slide 76: FACTORS AFFECTING COMPACTION
Water Content
Amount of Compaction
Method of Compaction
Type of Soil
Addition of Admixtures

## Slide 77: EFFECT OF WATER CONTENT
With increase in water content, compacted density increases up to a stage, beyond which compacted density decreases.
The maximum density achieved is called MDD and the corresponding water content is called OMC.
At lower water contents than OMC, soil particles are held by the force that prevents the development of diffused double layer leading to low inter-particle repulsion.
Increase in water results in expansion of double layer and reduction in net attractive force between particles. Water replaces air in void space

## Slide 78
Particles slide over each other easily increasing lubrication, helping in dense packing.
After OMC is reached, air voids remain constant. Further increase in water, increases the void space, thereby decreasing dry density.

## Slide 79: EFFECT OF AMOUNT OF COMPACTION
As discussed earlier, effect of increasing compactive effort is to increase MDD And reduce OMC (Evident from Standard & Modified Proctor’s Tests).
However, there is no linear relationship between compactive effort and MDD.

## Slide 80: EFFECT OF METHOD OF COMPACTION
The dry density achieved by the soil depends on the following characteristics of compacting method.
Weight of compacting equipment
Type of compaction
Area of contact of
Time of exposure
Each of these approaches will yield different compactive effort.

## Slide 81: EFFECT OF TYPE OF SOIL
Maximum density achieved depends on type of
Coarse grained soil achieves higher density at lower water content and fine grained soil achieves lesser density, but at higher water content
Further, suitability of a particular method depends on type of soil.

## Slide 83: EFFECT OF ADDITION OF ADMIXTURES
Stabilizing agents are the admixtures added to soil.
The effect of adding these admixtures is to stabilize the soil.
In many cases they accelerate the process of densification.

## Slide 84: EFFECT OF COMPACTION ON SOIL PROPERTIES
Density
Shear strength
Permeability
Bearing Capacity
Settlement
Soil Structure
Pore Pressure
Stress Strain characteristics
Swelling & Shrinkage

## Slide 85: INFLUENCE ON DENSITY
Effect of compaction is to reduce the voids by expelling out air.
This results in increasing the dry density of soil mass.

## Slide 86: INFLUENCE ON SHEAR STRENGTH
Increase the number of contacts resulting in increased shear strength, especially in granular soils.
In clays, shear strength depends on dry density, moulding water content, soil structure, method of compaction, strain drainage condition etc.
Shear strength of cohesive soils compacted dry of optimum (flocculated structure) will be higher than those compacted wet of optimum (dispersed structure).

## Slide 87: INFLUENCE ON SHEAR STRENGTH

## Slide 88: EFFECT OF COMPACTION ON PERMEABILITY
Increased dry density, reduces the void space, thereby reducing permeability.
At same density, soil compacted dry of optimum is more permeable.
At same void ratio, soil with bigger particle size is more permeable.
Increased compactive effort reduces permeability.

## Slide 89: EFFECT ON BEARING CAPACITY
Increase in compaction increases the density and number of contacts between soil particles.
This results in increased bearing capacity which is a function of density.

## Slide 90: EFFECT ON SETTLEMENT
Compaction increases density and decreases void ratio, this results in reduced settlement.
Both elastic settlement and consolidation settlement are reduced.
Soil compacted dry of optimum experiences greater compression than that compacted wet of optimum.

## Slide 91: EFFECT ON COMPRESSIBILITY
Optimum shows more compressibility than that on dry side. But at higher pressure, behavior is similar.

## Slide 92: EFFECT ON SOIL STRUCTURE
In fine grained soil
1. On dry side of optimum, the structure is flocculated. The particles repel and density is less.
2. Addition of water increases lubrication and transforms the structure into dispersed structure
In coarse grained soil, single grained structure is maintained
In composite soil, behaviour depends on composition.

## Slide 94: EFFECT ON PORE PRESSURE
Clayey soil compacted dry of optimum develops less pore water pressure than that compacted wet of optimum at the same density at low strains.
However, at higher strains the effect is the same in both the cases.

## Slide 95: EFFECT ON STRESS STRAIN CHARACTERISTICS
The strength and modulus of elasticity of soil on the dry side of optimum will always be better than on the wet side for the same density.
Soil compacted dry of optimum shows brittle failure and that compacted on wet side experiences increased strain

## Slide 96: EFFECT ON SWELL SHRINK ASPECT
The effect of compaction is to reduce the void space. Hence the swelling and shrinkage are enormously reduced.
Further, soil compacted dry of optimum exhibits greater swell and swell pressure than that compacted on wet side because of random orientation and deficiency in water.

## Slide 97: FIELD COMPACTION EQUIPMENTS
The different types of field compacting equipments are:-
Smooth Wheeled Steel Drum Rollers
Pneumatic Tyred Rollers
Sheepsfoot Rollers
Impact Rollers
Vibrating Rollers
Hand Operated Vibrating Plate & rammer compactors.

## Slide 98: SMOOTH WHEELED STEEL DRUM ROLLERS
Capacity 20 kN to 200 kN
Self propelled or towed
Suitable for well graded sand, gravel, silt of low plasticity
Unsuitable for uniform sand, silty and soft clay

## Slide 100: PNEUMATIC TYRED ROLLERS
Usually two axles carrying rubber tyred wheels for full width of track
Dead load (water) is added to give a weight of 100 to 400 kN
Suitable for most coarse & fine soils
Unsuitable for very soft clay & highly variable soil

## Slide 102: SHEEPSFOOT ROLLERS
Self propelled or towed
Drum fitted with projecting club shaped feet to providing kneading action
Weight of 50 to 80 kN
Suitable for fine grained soil, sand & gravel with considerable fines

## Slide 104: IMPACT ROLLERS
Compaction by static pressure combined with impact of pentagonal roller
Higher impact energy breaks soil lump and provides kneading action

## Slide 105: VIBRATING ROLLERS
Roller drum fitted with vibratory motion
Levels and smoothens ruts
Suitable for cohensionless soils

## Slide 106: PLATE & RAMMER COMPACTORS
It is used for backfilling trenches, smaller constructions and less accessible locations

## Slide 107: COMPACTION CONTROL IN FIELD
There are many variables which control the vibratory compaction or densification of soils :-
Characteristics of the compactor
Characteristics of the soil
Construction procedures

## Slide 108
Characteristics of the compactor:
Mass, size
Operating frequency and frequency range
Characteristics of the soil:
Initial density
Grain size and shape
Water content
Construction procedures:
Number of passes of the roller
Lift thickness
Frequency of operation vibrator
Towing speed

## Slide 109: PROCTOR NEEDLE

## Slide 110
Used for rapid determination of water content of soil in field.
Rapid moisture meter is used as an alternative.
Proctor’s needle consists of a point, attached to graduated needle shank and spring loaded plunger.
Varying cross sections of needle points are available.
The penetration force is read on stem at top.
To use the needle in field Calibration in done on the specific soil in lab and calibration curve is prepared and the curve is used in the field to determine placement water content.

## Slide 112: DEGREE OF COMPACTION
Relative compaction or degree of compaction
It is a statistical result based on 47 soil samples.
Typical required RC > = 95%.

## Slide 113: DYNAMIC COMPACTION
This is used to compact both cohesive and cohesion less soils.
In this compaction a crane is used to lift a concrete or steel block weighing upto 500 kN upto a height of 40 to 50 m.
From this height the block is allowed to fall freely on the ground surface.
The process is repeated over the area.
Soil at the surfaces is disturbed. It is then refilled and leveled. Depth of compaction is upto 12m.
This method is quick & produces uniform settlement.

## Slide 115: VIBROFLOATATION
It is used for compacting thick deposit of loose sandy soil upto 30 m depth.
The vibrofloat consists of cylindrical tube about 2m in diameter and fitted with water jet at the top and bottom. It contains a eccentric weight which develops a horizontal vibratory motion.
Vibrofloat is sunk into the ground & it vibrates laterally and causes compaction of soil in the horizontal direction.
The water from lower jet transfer to the top jet & pressure is reduced. So that the jet is enough to carry sand poured at the top to the bottom of the hole.

## Slide 116
As vibrofloat is slowly rise to the surface the additional sand is dropped into space around vibrofloat.
By raising the vibrofloat in stage, simultaneously backfilling the entire depth of soil is compacted.

## Slide 117
A laboratory compaction test on a soil having G = 2.68 gave a maximum dry density of 17.85 kN/m3 and the moisture content 17%. Find the degree of saturation, air content & % air voids @ the maximum dry density. Also find the theoretical maximum dry density with respect to zero air voids at optimum moisture content.
G = 2.68
W = 17%
γd = 17.85 kN/m3

## Slide 118
(i) Degree of Saturation

## Slide 119
(ii) Air Content
(iii) % Air Voids

## Slide 120
(iii) % Air Voids, = 0 , S =100%

## Slide 121
The following observations were taken during a control test to measure the density of compacted fill.
Weight of compacted soil excavated from the pit = 8.8 N
Weight of sand filling the pit = 6.8 N
Bulk density of sand = 14.5 kN/m3
Water content of natural soil = 15%
Compute the wet & dry density of compacted soil.

## Slide 122
Volume of compacted soil

## Slide 123
Bulk Density of compacted soil

## Slide 124
Dry Density of compacted soil

## Slide 125
A saturated proctor test was performed on a soil sample of G = 2.7 with the following results. Maximum dry density γd = 17.65 kN/m3, OMC = 16%. If the compaction effect was increased so that the maximum dry density increases to γd = 18.83 kN/m3. Assuming the same degree of saturation, what should be the corresponding OMC.
Case 1: G = 2.7, γd = 17.65 kN/m3 & OMC = 16%
Case 2: γd = 18.83 kN/m3, OMC = ?

## Slide 126
Case 1:

## Slide 127
Case 2:

## Slide 128
Following are the results of standard compaction test on a soil.
Plot dry unit weight versus water content relationship & get the maximum dry unit weight & OMC. Show 70% & 100 % saturation lines on the plot. Take, G = 2.65.
Water content (%) | 13.5 | 20.2 | 25.0 | 35.0 | 41.5
Bulk density in kN/m3 | 16.3 | 19.4 | 18.80 | 18.0 | 17.20

## Slide 129
Water content (%) | 13.5 | 20.2 | 25.0 | 35.0 | 41.5
Bulk density in kN/m3 | 16.3 | 19.4 | 18.80 | 18.0 | 17.20
Dry density, γd in kN/m3 | 14.36 | 16.14 | 15.04 | 13.33 | 12.15
Dry density, γd in kN/m3 (For, S = 70%) | 17.20 | 14.73 | 13.36 | 11.18 | 10.11
Dry density, γd in kN/m3 (For, S = 100%) | 19.14 | 16.93 | 15.63 | 13.49 | 12.38

## Slide 131
The following data refer to I.S light compaction test in a cylindrical mould of 1000 cc volume.
Specific gravity of solids is 2.7. Plot the compaction curve and obtained maximum dry unit weight and optimum moisture content. Plot zero air void line and 80% saturation line.
Water content (%) | 10 | 12 | 14.3 | 16 | 18.3
Weight of wet sample (N) | 19.63 | 21.37 | 21.93 | 21.68 | 21.14